## Slide 1: Updates 8/4/20
Akash Levy

## Slide 2: Overview
Sweep plot for FPPV
Sweep plots for VWL and VBL
Retention distribution plots
Retention BER plot
ISPP optimization results
SDCFC optimization results
ISPP/FPPV evaluation on chip 1

## Slide 3: TODO List (In Order)
Optimize ISPP
Evaluate ISPP on 4K more cells and add to previously collected data
Optimize SDR SL over 256 cells
  Sweep step size from 0.02 to 0.22 in steps of 0.04 (6)
  Sweep start voltage from 0 to 1 in steps of 0.2 (6)
  Total: 36
Optimize SDR BL over 256 cells
  Sweep step size from 0.02 to 0.22 in steps of 0.04 (6)
  Sweep start voltage from 0 to 1.2 in steps of 0.4 (4)
  Total: 24
Optimize SDR SL over 256 cells
  Sweep step size from 0.02 to 0.22 in steps of 0.04 (6)
  Sweep start voltage from 0 to 1.2 in steps of 0.4 (4)
  Total: 24
Evaluate SDCFC on 8K cells (addr 10240 -> 8K)
Redo sweeps on 50 cells with 10 per cell using proper step sizes
  7.5 kOhm slope measurement
  0.05V step size starting from 0V
Evaluate FPPVv2 on 8K cells (with 2000 attempts)
Endurance testing
2bpc repeat all steps above
Chip 2
  Do FPPV sweep and find coarse settings
  Redo evaluation on 8K cells
  Redo endurance testing

## Slide 4: Sweep Plots
Slope comparisons for different knobs, and FPPV results

## Slide 5: Sweep Plots: FPPV VWL Chip 1

## Slide 6: Sweep Plots: SET VWL

## Slide 7: Sweep Plots: RESET VWL

## Slide 8: Sweep Plots: SET VBL

## Slide 9: Sweep Plots: RESET VSL

## Slide 10: 3bpc Algorithms
Optimization and experimental results

## Slide 11: Resistance Ranges
 | Rmin | Rmax | Rwmin | Rwmax
Range 0 | N/A | 4.3k | N/A | 4.2k
Range 1 | 4.38k | 4.75k | 4.54k | 4.58k
Range 2 | 4.84k | 5.3k | 5.04k | 5.09k
Range 3 | 5.42k | 6.01k | 5.67k | 5.73k
Range 4 | 6.16k | 6.99k | 6.51k | 6.59k
Range 5 | 7.19k | 8.9k | 7.71k | 7.87k
Range 6 | 9.2k | 25k | 11.42k | 11.93k
Range 7 | 20k | N/A | 80k | N/A

## Slide 12: ISPP Optimization Results

## Slide 13: VBL Step Size Optimization

## Slide 14: VSL Step Size Optimization

## Slide 15: Optimization Parameters
 | VBL Start (V) | VBL Step (V) | VSL Start (V) | VSL Step (V)
Range 0 | 2 | 0.3 | N/A | N/A
Range 1 | 0 | 0.14 | 0 | 0.14
Range 2 | 0 | 0.1 | 0 | 0.1
Range 3 | 0 | 0.1 | 0 | 0.1
Range 4 | 0 | 0.1 | 0 | 0.1
Range 5 | 0 | 0.06 | 0 | 0.06
Range 6 | 0 | 0.06 | 0 | 0.1

## Slide 16: Algorithm evaluation on 4 WLs: chip 1

## Slide 17: Algorithm evaluation on 4 WLs: chip 2

## Slide 18: 3bpc algorithm evaluation on 4 WLs
Chip # | Cycles | SDCFC | ISPP | FPPV
1 | 300 | 36.44 | 86.10 | >90
2 | 300 | 35.88 | >90 | >90
1 | 8k | 35.19 | >90 | >90
2 | 8k | TODO | >90 | >90
Notes: 92.95 for chip 2 ISPP

## Slide 19: 2bpc Algorithms
Optimization and experimental results

## Slide 20: Resistance Ranges
 | Rmin | Rmax | Rwmin | Rwmax
Range 0 | N/A | 5.10k | N/A | 5.00k
Range 1 | 5.38k | 6.48k | 5.77k | 6.01k
Range 2 | 6.93k | 12.00k | 8.51k | 9.31k
Range 3 | 20.00k | N/A | 80k | N/A

## Slide 21: ISPP Optimization Results

## Slide 22: VBL Step Size Optimization

## Slide 23: VSL Step Size Optimization

## Slide 24: Optimization Parameters
 | VBL Start (V) | VBL Step (V) | VSL Start (V) | VSL Step (V)
Range 0 | 2 | 0.3 | N/A | N/A
Range 1 | 0.6 | 0.18 | 0.6 | 0.26
Range 2 | 0.8 | 0.1 | 0.6 | 0.34

## Slide 25: Algorithm evaluation on 4 WLs: chip 1

## Slide 26: Algorithm evaluation on 4 WLs: chip 2

## Slide 27: 2bpc algorithm evaluation on 4 WLs
Chip # | Cycles | SDCFC | ISPP | FPPV
1 | 300 | 8.52 | 20.51 | 15.75
2 | 300 | 8.50 | 21.62 | 16.83
1 | 8k | 9.56 | >25 | >25
2 | 8k | 9.39 | >25 | >25

## Slide 28: Retention
Distributions (empirical and predicted)

## Slide 29: Combined Distribution Plot

## Slide 30: Retention model plot

## Slide 31: Retention BER plot

## Slide 32: Comparison Table

## Slide 33: Comparison References

## Slide 34: Backup
Things we will show only if reviewers or co-authors ask

## Slide 35: 3bpc Pre-Optimization Parameters
 | VBL Start (V): Seed | VBL Step (V): Seed | VSL Start (V) | VSL Step (V)
Range 0 | 0.4 | 0.04 | N/A | N/A
Range 1 | 0.4 | 0.04 | 0.6 | 0.18
Range 2 | 0.4 | 0.04 | 0.2 | 0.22
Range 3 | 0.4 | 0.04 | 0.4 | 0.14
Range 4 | 0.4 | 0.04 | 0.4 | 0.14
Range 5 | 0.4 | 0.04 | 0.4 | 0.14
Range 6 | 0.4 | 0.04 | 0.4 | 0.14

## Slide 36: 2bpc Pre-Optimization Parameters
 | VBL Start (V): Seed | VBL Step (V): Seed | VSL Start (V) | VSL Step (V)
Range 0 | 2 | 0.3 | N/A | N/A
Range 1 | 0 | 0.04 | 0 | 0.16
Range 2 | 0 | 0.04 | 0 | 0.1

## Slide 37: BER Plot at 100 Pulses

## Slide 38: Retention BER plot full

## Slide 39: Combined Pre/Post-Bake Distribution Plot
(a)
(b)

## Slide 40: VBL Optimization
Optimal Parameter Set
Step Size: 0.1V
Start Voltage: 0V

## Slide 41: VSL Optimization 1

## Slide 42: VSL Optimization 2
Optimal Parameter Set
Step Size: 0.1V
Start Voltage: 0V

## Slide 43: Algorithm Parameters