## Slide 1: Updates 5/11/20
Akash Levy

## Slide 2: Overview
New BL/WL sweep with 10 cells
New sigma-mu and sigma-median plots
SDR fixed implementation
Optimization of ISPP
Optimal BL/WL voltages for FPPV and SDR
New resistance ranges
Optimization of SDR

## Slide 3: Old BL/WL Sweeps
NOTE: >2𝜎 outliers removed

## Slide 4: New BL/WL Sweeps
NOTE: >2𝜎 outliers removed

## Slide 5: Sigma-Mu Plot
METHODOLOGY:
Filter data for 1.5 V < BLV ≤ 3 V
Filter data for 2 V < WLV ≤ 3 V
Filter data for PW = 100ns
Group by WLV and BLV
Remove outliers based on 2σ
Find non-dominated front (pareto front)

## Slide 6: Sigma-Median Plot
METHODOLOGY:
Filter data for 1.5 V < BLV ≤ 3 V
Filter data for 2 V < WLV ≤ 3 V
Filter data for PW = 100ns
Group by WLV and BLV
Remove outliers based on 2σ
Find non-dominated front (pareto front)

## Slide 7: Old Optimal BL/WL from pareto front
 | BLV (V) | WLV (V)
Range 0 | 3.3 | 3
Range 1 | 2.7 | 2.84
Range 2 | 2.9 | 2.65
Range 3 | 2.7 | 2.58
Range 4 | 3 | 2.48
Range 5 | 2.5 | 2.42
Range 6 | 2.75 | 2.3
Range 7 | N/A | N/A

## Slide 8: New Optimal BL/WL from pareto front
 | BLV (V) | WLV (V)
Range 0 | 3.3 | 3
Range 1 | 2.7 | 2.93
Range 2 | 2.55 | 2.66
Range 3 | 1.8 | 2.61
Range 4 | 1.65 | 2.55
Range 5 | 2.5 | 2.34
Range 6 | 2.05 | 2.29
Range 7 | N/A | N/A

## Slide 9: SDR Fixed Implementation
RESET pulse
Check if in range
Optimal SET pulse
Check if in RMM range, else restart
RMM defined by RM of level above and Rm of level below
SET tuning if resistance too high, RESET tuning if resistance too low
Sweep up BLV for SET
Sweep up SLV for RESET
Restart if fail

## Slide 10: ISPP Algorithm
Start with WLV = 2.1V
Increase WLV by step size
Pulse until in range, RESET if gone past
Step size swept from 0.01V to 0.15V
Key metrics
  Avg. # of attempts needed
  Avg. # of total pulses needed
  (Distribution of pulses needed)
  (Per bin and overall)
Best step size: 0.06V, success: 99.66%
Mean pulses: 8.95, Stdev pulses: 7.75
Mean resets: 1.86, Stdev resets: 1.96

## Slide 11: ISPP Algorithm
Start with WLV = 2.1V
Increase WLV by step size
Pulse until in range, RESET if gone past
Step size swept from 0.01V to 0.15V
Key metrics
  Avg. # of attempts needed
  Avg. # of total pulses needed
  (Distribution of pulses needed)
  (Per bin and overall)
Best step size: 0.06V, success: 99.66%
Mean pulses: 8.95, Stdev pulses: 7.75
Mean resets: 1.86, Stdev resets: 1.96

## Slide 12: FPPV Algorithm
Success: 96.0%
Mean pulses: 7.16, Stdev pulses: 9.32

## Slide 13: SDR Algorithm
Success: 96.0%
Mean pulses: 7.16, Stdev pulses: 9.32

## Slide 14: EAG Success Rates

## Slide 15: EAG Pulse Counts

## Slide 16: Backup Slides
New data with the 100 cells
Good figures for if we need to make the paper longer

## Slide 17: FORMing
100 cells FORMed
PW = 1000ns, WL = 2V
BL voltage from 0-5V in steps of 0.05V
Aim for medium post-FORM resistance
Medium post-FORM resistance
  6-7kOhm
No over-FORM, no under-FORM

## Slide 18: Cell Cycling
300 cycles per cell (100 cells)
Two pulses per cycle per cell
SET pulse
  PW=100ns, BLV=3.3V, WLV=3V
RESET pulse
  PW=100ns, SLV=2.3V, WLV=4V
Maximum SET resistance across cells, minimized over all
  Lower Bound: 5.16 kΩ