## Slide 1: Updates 8/15/20
Akash Levy

## Slide 2: Overview
Sweep plot for FPPV
Sweep plots for VWL and VBL
Retention distribution plots
Retention BER plot
ISPP optimization results
SDCFC optimization results
ISPP/FPPV evaluation on chip 1

## Slide 3: Sweep Plots
Slope comparisons for different knobs, and FPPV results

## Slide 4: Sweep Plots: FPPV VWL Chip 1

## Slide 5: Sweep Plots: SET VWL

## Slide 6: Sweep Plots: RESET VWL

## Slide 7: Sweep Plots: SET VBL

## Slide 8: Sweep Plots: RESET VSL

## Slide 9: 3bpc Algorithms
Optimization and experimental results

## Slide 10: Resistance Ranges
 | Rmin | Rmax | Rwmin | Rwmax
Range 0 | N/A | 4.3k | N/A | 4.2k
Range 1 | 4.38k | 4.75k | 4.54k | 4.58k
Range 2 | 4.84k | 5.3k | 5.04k | 5.09k
Range 3 | 5.42k | 6.01k | 5.67k | 5.73k
Range 4 | 6.16k | 6.99k | 6.51k | 6.59k
Range 5 | 7.19k | 8.9k | 7.71k | 7.87k
Range 6 | 9.2k | 25k | 11.42k | 11.93k
Range 7 | 20k | N/A | 80k | N/A

## Slide 11: ISPP Optimization Results

## Slide 12: VBL Step Size Optimization

## Slide 13: VSL Step Size Optimization

## Slide 14: Optimization Parameters
 | VBL Start (V) | VBL Step (V) | VSL Start (V) | VSL Step (V)
Range 0 | 2 | 0.3 | N/A | N/A
Range 1 | 0 | 0.14 | 0 | 0.14
Range 2 | 0 | 0.1 | 0 | 0.1
Range 3 | 0 | 0.1 | 0 | 0.1
Range 4 | 0 | 0.1 | 0 | 0.1
Range 5 | 0 | 0.06 | 0 | 0.06
Range 6 | 0 | 0.06 | 0 | 0.1

## Slide 15: Algorithm evaluation on 4 WLs: chip 1

## Slide 16: Algorithm evaluation on 4 WLs: chip 2

## Slide 17: 3bpc algorithm evaluation on 4 WLs
Chip # | Cycles | SDCFC | ISPP | FPPV
1 | 300 | 36.44 | 86.10 | >90
2 | 300 | 35.88 | >90 | >90
1 | 8k | 35.19 | >90 | >90
2 | 8k | 35.53 | >90 | >90
Notes: 92.95 for chip 2 ISPP

## Slide 18: 2bpc Algorithms
Optimization and experimental results

## Slide 19: Resistance Ranges
 | Rmin | Rmax | Rwmin | Rwmax
Range 0 | N/A | 5.10k | N/A | 5.00k
Range 1 | 5.38k | 6.48k | 5.77k | 6.01k
Range 2 | 6.93k | 12.00k | 8.51k | 9.31k
Range 3 | 20.00k | N/A | 80k | N/A

## Slide 20: ISPP Optimization Results

## Slide 21: VBL Step Size Optimization

## Slide 22: VSL Step Size Optimization

## Slide 23: Optimization Parameters
 | VBL Start (V) | VBL Step (V) | VSL Start (V) | VSL Step (V)
Range 0 | 2 | 0.3 | N/A | N/A
Range 1 | 0.6 | 0.18 | 0.6 | 0.26
Range 2 | 0.8 | 0.1 | 0.6 | 0.34

## Slide 24: Algorithm evaluation on 4 WLs: chip 1

## Slide 25: Algorithm evaluation on 4 WLs: chip 2

## Slide 26: 2bpc algorithm evaluation on 4 WLs
Chip # | Cycles | SDCFC | ISPP | FPPV
1 | 300 | 8.52 | 20.51 | 15.75
2 | 300 | 8.50 | 21.62 | 16.83
1 | 8k | 9.56 | >25 | >25
2 | 8k | 9.39 | >25 | >25

## Slide 27: Retention
Distributions (empirical and predicted)

## Slide 28: Combined Distribution Plot

## Slide 29: Retention model plot

## Slide 30: Retention BER plot

## Slide 31: Comparisons
For establishing the context surrounding our work

## Slide 32: Comparison Table (Full)
Ref. | Algo. Family | Array-Level | Bits-per-cell | # of Cells Measured | Efficient Ranges/Gaps | Endurance | Retention
This work | SDCFC | Yes | 3 | 16,384 | Yes | Yes | High-temp Array-level
[2] | FPPV | No | 2 | Single cell | No | No | None
[3] | ISPP | Yes | 2 | Single cell | No | Yes | High-temp Single-cell
[4] | FPPV | Yes | 3 | 7,746 | Yes | Yes | None
[11] | ISPP | Yes | 2 | 4,096 | No | Yes | High-temp Array-level
[12] | ISPP | No | 4 | Single cell | No | No | Low-temp Single-cell

## Slide 33: Comparison References
Toward Reliable Multi-Level Operation in RRAM Arrays: Improving Post-Algorithm Stability and Assessing Endurance/Data Retention
Optimized Method for Low-Energy and Highly Reliable Multibit Operation in a HfO2-Based Resistive Switching Device
Fully “Erase-free” Multi-Bit Operation in HfO2‐Based Resistive Switching Device
A multi-level 40nm WOx resistive memory with excellent reliability
Demonstration of low power 3-bit multilevel cell characteristics in a TaOx-based RRAM by stack engineering
A novel program- verify algorithm for multi-bit operation in HfO2 RRAM
Four-bits-per-cell operation in an HfO2-based resistive switching device

## Slide 34: Backup
Things we will show only if reviewers or co-authors ask

## Slide 35: 3bpc Pre-Optimization Parameters
 | VBL Start (V): Seed | VBL Step (V): Seed | VSL Start (V) | VSL Step (V)
Range 0 | 0.4 | 0.04 | N/A | N/A
Range 1 | 0.4 | 0.04 | 0.6 | 0.18
Range 2 | 0.4 | 0.04 | 0.2 | 0.22
Range 3 | 0.4 | 0.04 | 0.4 | 0.14
Range 4 | 0.4 | 0.04 | 0.4 | 0.14
Range 5 | 0.4 | 0.04 | 0.4 | 0.14
Range 6 | 0.4 | 0.04 | 0.4 | 0.14

## Slide 36: 2bpc Pre-Optimization Parameters
 | VBL Start (V): Seed | VBL Step (V): Seed | VSL Start (V) | VSL Step (V)
Range 0 | 2 | 0.3 | N/A | N/A
Range 1 | 0 | 0.04 | 0 | 0.16
Range 2 | 0 | 0.04 | 0 | 0.1

## Slide 37: BER Plot at 100 Pulses

## Slide 38: Combined Pre/Post-Bake Distribution Plot
(a)
(b)

## Slide 39: VBL Optimization
Optimal Parameter Set
Step Size: 0.1V
Start Voltage: 0V

## Slide 40: VSL Optimization 1

## Slide 41: VSL Optimization 2
Optimal Parameter Set
Step Size: 0.1V
Start Voltage: 0V

## Slide 42: Algorithm Parameters