## Slide 1: Z58U1 Drift
Investigated Drift behavior.
  Performed multiple successive read events and samples with different time delays.
  Large Drift was only observed after the First Read Event
  More delay before first Read Event caused same amount of drift.
  Multiple Samples within the same read event do not appear to show drift (only measurement noise).
  Switching between PMU and digital driver appears to cause “set” like event, which causes subsequent reads to have new value.
  Rewrote Read routine to reduce glitching and hopefully solve drift problem.
Note: all plots are using the “Coarse Set Discovery” routine, so each point is actually the median of 20trials.

## Slide 2: Original Drift Issue Observed
Filter Settings
SDR_Tuning_20200110_161558.data_unpivot
- FileName: (ZE8U1_WL0C105_20200127_111125.stdf)
- Address: (420, 804)
- Sequencer: (coarsesetdiscovery)
- vWLS: (1.491 <= vWLS <= 1.637)
First Read event
Second Read Event 20ms delayed
Drift
Based on experiment, this drift is due to Sequential read events rather than the time delay between successive measurements.

## Slide 3: Improved Read Routine.
Filter Settings
SDR_Tuning_20200110_161558.data_unpivot
- FileName: (.\ZE8U1_DriftExp_FastRead_20200128_103444.stdf)
- Address: (420, 804)
- Sequencer: (coarsesetdiscovery)
- vWLS: (1.491 <= vWLS <= 1.637)
10 full read events at different delays were performed.
New routine no longer shows drift due to successive events.

## Slide 4: SDR Programming
2020.02.06

## Slide 5: About
ZE8U2
Started by testing 256cells
😥 Only 28cells passed Dynamic Form/Set/Reset routines with the chosen conditions and went on to try the SDR programming.
Range0 and Range7 Successfully programmed for all 28bits.
😫Many SDR programming attempts for Range1-6 failed.

## Slide 6: SDR Resistance
28 cells, 10 trials per cell at each range.

## Slide 7: SDR State Counts
At 50pulses the programming attempt is considered a failure.
Value vs. Wordline, Column, Trial
Wordline, Column, Trial
V
a
l
u
e
7
9
1
3
5
7
9
1
6
25
3
2
3
4
32
3
0
1
2
3
5
7
9
1
3
5
7
9
1
6
25
3
2
3
4
32
3
0
1
2
3
5
7
9
1
3
5
7
9
1
6
25
3
2
3
4
32
3
0
1
2
3
5
7
9
1
3
5
7
9
1
6
25
3
2
3
4
32
3
0
1
2
3
5
7
9
1
3
5
7
9
1
6
25
3
2
3
4
32
3
0
1
2
3
5
7
9
1
3
5
7
9
1
6
25
3
2
3
4
32
3
0
1
2
3
5
7
9
1
3
5
7
9
1
6
25
3
2
3
4
32
3
0
1
2
3
5
7
9
1
3
5
7
9
1
6
25
3
2
3
4
32
3
0
1
2
3
5
50
45
40
35
30
25
20
15
10
5
0
Pulse Count
0
1
2
3
4
5
6
7
1.15
1.15
1.15
1.15
1.15
1.15
1.15
1.15
1.15
14.07
14.07
14.07
14.07
14.07
14.07
14.07
14.07
14.07
22.25
22.25
22.25
22.25
22.25
22.25
22.25
22.25
22.25
20.75
20.75
20.75
20.75
20.75
20.75
20.75
20.75
20.75
20.26
20.26
20.26
20.26
20.26
20.26
20.26
20.26
20.26
15.29
15.29
15.29
15.29
15.29
15.29
15.29
15.29
15.29
7.75
7.75
7.75
7.75
7.75
7.75
7.75
7.75
7.75
0.16
0.16
0.16
0.16
0.16
0.16
0.16
0.16
0.16
Data table:
SDR_Tuning_20200110_16
Trellis by
Range
Measurement
Marker by
(Row Number)
Color by
FileName
.\ZE8U2_SDR_1.6_Step
…