## Slide 1: Updates 7/18/20
Akash Levy

## Slide 2: Overview
Sweep plot for FPPV
Sweep plots for VWL and VBL
Retention distribution plots
Retention BER plot
ISPP optimization results
SDCFC optimization results
ISPP/FPPV evaluation on chip 1

## Slide 3: TODO List (In Order)
Evaluate ISPP on 4K more cells and add to previously collected data
Optimize SDR SL over 256 cells
  Sweep step size from 0.02 to 0.22 in steps of 0.04 (6)
  Sweep start voltage from 0 to 1 in steps of 0.2 (6)
  Total: 36
Optimize SDR BL over 256 cells
  Sweep step size from 0.02 to 0.22 in steps of 0.04 (6)
  Sweep start voltage from 0 to 1.2 in steps of 0.4 (4)
  Total: 24
Optimize SDR SL over 256 cells
  Sweep step size from 0.02 to 0.22 in steps of 0.04 (6)
  Sweep start voltage from 0 to 1.2 in steps of 0.4 (4)
  Total: 24
Evaluate SDCFC on 8K cells (addr 10240 -> 8K)
Evaluate FPPVv2 on 8K cells (with 2000 attempts)
Redo sweeps on 50 cells with 10 per cell using proper step sizes
  7.5 kOhm slope measurement
Endurance testing
2bpc repeat

## Slide 4: Sweep Plots: FPPV VWL

## Slide 5: Sweep Plots: VWL SET/RST (REDO STEP)
Notes: Slope @ resistance is the key!!!

## Slide 6: Sweep Plots: VBL/VSL SET/RST (REDO STEP)
Notes: Slope @ resistance is the key!!!

## Slide 7: ISPP Optimization Results

## Slide 8: Algorithm evaluation on 4 WLs (TODO)

## Slide 9: VSL Step Size Optimization Initial
For all ranges:
  Using VBL step size of 0.04V
  Using VBL start voltage of 0.4V

## Slide 10: VBL Step Size Optimization

## Slide 11: VSL Step Size Optimization Final

## Slide 12: Algorithm evaluation on 4 WLs (TODO)
Chip # | Cycles | ISPP | FPPV | SDCFC
1 | 300 | 86.10 |  | 35.71
2 | 300 |  |  | 
1 | 10k |  |  | 
2 | 10k |  |  | 

## Slide 13: Resistance Ranges
 | Rmin | Rmax | Rwmin | Rwmax
Range 0 | N/A | 4.3k | N/A | 4.2k
Range 1 | 4.38k | 4.75k | 4.54k | 4.58k
Range 2 | 4.84k | 5.3k | 5.04k | 5.09k
Range 3 | 5.42k | 6.01k | 5.67k | 5.73k
Range 4 | 6.16k | 6.99k | 6.51k | 6.59k
Range 5 | 7.19k | 8.9k | 7.71k | 7.87k
Range 6 | 9.2k | 25k | 11.42k | 11.93k
Range 7 | 20k | N/A | 80k | N/A

## Slide 14: Resistance Ranges
 | VBL Start (V) | VBL Step (V) | VSL Start (V) | VSL Step (V)
Range 0 | 2 | 0.3 | N/A | N/A
Range 1 | 0.14 | 0.14 | 0.18 | 0.6
Range 2 | 0.1 | 0.1 | 0.22 | 0.2
Range 3 | 0.1 | 0.1 | 0.14 | 0.4
Range 4 | 0.1 | 0.1 | 0.14 | 0.4
Range 5 | 0.06 | 0.06 | 0.14 | 0.4
Range 6 | 0.06 | 0.06 | 0.14 | 0.4

## Slide 15: Combined Pre/Post-Bake Distribution Plot

## Slide 16: Retention model plot

## Slide 17: Retention BER plot

## Slide 18: Retention BER plot full

## Slide 19: VBL Optimization
Optimal Parameter Set
Step Size: 0.1V
Start Voltage: 0V (adj. to 0.1V)
Mean Pulses: 38.4, Success: 99.6%

## Slide 20: VSL Optimization
Optimal Parameter Set
Step Size: 0.14V
Start Voltage: 0.4V
Success Rate: 99.6%