## Slide 1: Updates 8/4/20
Akash Levy

## Slide 2: Overview
Sweep plot for FPPV
Sweep plots for VWL and VBL
Retention distribution plots
Retention BER plot
ISPP optimization results
SDCFC optimization results
ISPP/FPPV evaluation on chip 1

## Slide 3: TODO List (In Order)
Optimize ISPP
Evaluate ISPP on 4K more cells and add to previously collected data
Optimize SDR SL over 256 cells
  Sweep step size from 0.02 to 0.22 in steps of 0.04 (6)
  Sweep start voltage from 0 to 1 in steps of 0.2 (6)
  Total: 36
Optimize SDR BL over 256 cells
  Sweep step size from 0.02 to 0.22 in steps of 0.04 (6)
  Sweep start voltage from 0 to 1.2 in steps of 0.4 (4)
  Total: 24
Optimize SDR SL over 256 cells
  Sweep step size from 0.02 to 0.22 in steps of 0.04 (6)
  Sweep start voltage from 0 to 1.2 in steps of 0.4 (4)
  Total: 24
Evaluate SDCFC on 8K cells (addr 10240 -> 8K)
Redo sweeps on 50 cells with 10 per cell using proper step sizes
  7.5 kOhm slope measurement
  0.05V step size starting from 0V
Evaluate FPPVv2 on 8K cells (with 2000 attempts)
Endurance testing
2bpc repeat all steps above
Chip 2
  Do FPPV sweep and find coarse settings
  Redo evaluation on 8K cells
  Redo endurance testing

## Slide 4: Sweep Plots
Slope comparisons for different knobs, and FPPV results

## Slide 5: Sweep Plots: FPPV VWL

## Slide 6: Sweep Plots: SET VWL

## Slide 7: Sweep Plots: RESET VWL

## Slide 8: Sweep Plots: SET VBL

## Slide 9: Sweep Plots: RESET VSL

## Slide 10: 3bpc Algorithms
Optimization and experimental results

## Slide 11: Resistance Ranges
 | Rmin | Rmax | Rwmin | Rwmax
Range 0 | N/A | 4.3k | N/A | 4.2k
Range 1 | 4.38k | 4.75k | 4.54k | 4.58k
Range 2 | 4.84k | 5.3k | 5.04k | 5.09k
Range 3 | 5.42k | 6.01k | 5.67k | 5.73k
Range 4 | 6.16k | 6.99k | 6.51k | 6.59k
Range 5 | 7.19k | 8.9k | 7.71k | 7.87k
Range 6 | 9.2k | 25k | 11.42k | 11.93k
Range 7 | 20k | N/A | 80k | N/A

## Slide 12: ISPP Optimization Results

## Slide 13: VBL Step Size Optimization

## Slide 14: VSL Step Size Optimization

## Slide 15: Optimization Parameters
 | VBL Start (V) | VBL Step (V) | VSL Start (V) | VSL Step (V)
Range 0 | 2 | 0.3 | N/A | N/A
Range 1 | 0 | 0.14 | 0 | 0.14
Range 2 | 0 | 0.1 | 0 | 0.1
Range 3 | 0 | 0.1 | 0 | 0.1
Range 4 | 0 | 0.1 | 0 | 0.1
Range 5 | 0 | 0.06 | 0 | 0.06
Range 6 | 0 | 0.06 | 0 | 0.1

## Slide 16: Algorithm evaluation on 4 WLs

## Slide 17: 3bpc algorithm evaluation on 4 WLs
Chip # | Cycles | SDCFC | ISPP | FPPV
1 | 300 | 36.44 | 86.10 | >90
2 | 300 | TODO | TODO | TODO
1 | 8k | 35.19 | >90 | >90
2 | 8k | TODO | TODO | TODO

## Slide 18: 2bpc Algorithms
Optimization and experimental results

## Slide 19: Resistance Ranges
 | Rmin | Rmax | Rwmin | Rwmax
Range 0 | N/A | 5.10k | N/A | 5.00k
Range 1 | 5.38k | 6.48k | 5.77k | 6.01k
Range 2 | 6.93k | 12.00k | 8.51k | 9.31k
Range 3 | 20.00k | N/A | 80k | N/A

## Slide 20: ISPP Optimization Results

## Slide 21: VBL Step Size Optimization

## Slide 22: VSL Step Size Optimization

## Slide 23: Optimization Parameters
 | VBL Start (V) | VBL Step (V) | VSL Start (V) | VSL Step (V)
Range 0 | 2 | 0.3 | N/A | N/A
Range 1 | 0.05 | 0.14 | 0 | 0
Range 2 | 0.05 | 0.14 | 0 | 0

## Slide 24: Algorithm evaluation on 4 WLs

## Slide 25: 2bpc algorithm evaluation on 4 WLs
Chip # | Cycles | SDCFC | ISPP | FPPV
1 | 300 | TODO | 20.21 | 14.38
2 | 300 | TODO | TODO | TODO
1 | 8k | TODO | TODO | TODO
2 | 8k | TODO | TODO | TODO

## Slide 26: Retention
Distributions (empirical and predicted)

## Slide 27: Combined Distribution Plot

## Slide 28: Retention model plot

## Slide 29: Retention BER plot

## Slide 30: Backup
Things we will show only if reviewers or co-authors ask

## Slide 31: 3bpc Pre-Optimization Parameters
 | VBL Start (V): Seed | VBL Step (V): Seed | VSL Start (V) | VSL Step (V)
Range 0 | 0.4 | 0.04 | N/A | N/A
Range 1 | 0.4 | 0.04 | 0.6 | 0.18
Range 2 | 0.4 | 0.04 | 0.2 | 0.22
Range 3 | 0.4 | 0.04 | 0.4 | 0.14
Range 4 | 0.4 | 0.04 | 0.4 | 0.14
Range 5 | 0.4 | 0.04 | 0.4 | 0.14
Range 6 | 0.4 | 0.04 | 0.4 | 0.14

## Slide 32: 2bpc Pre-Optimization Parameters
 | VBL Start (V): Seed | VBL Step (V): Seed | VSL Start (V) | VSL Step (V)
Range 0 | 2 | 0.3 | N/A | N/A
Range 1 | 0 | 0.04 |  | 
Range 2 | 0 | 0.04 |  | 

## Slide 33: Retention BER plot full

## Slide 34: Combined Pre/Post-Bake Distribution Plot
(a)
(b)

## Slide 35: VBL Optimization
Optimal Parameter Set
Step Size: 0.1V
Start Voltage: 0V

## Slide 36: VSL Optimization 1

## Slide 37: VSL Optimization 2
Optimal Parameter Set
Step Size: 0.1V
Start Voltage: 0V

## Slide 38: Algorithm Parameters