## Slide 1: Updates 7/6/20
Akash Levy

## Slide 2: Overview
Retention results
Updated SDR algorithm
Questions
Retention figures

## Slide 3: Retention Results
Before baking: programmed several times until BER goes to 0
Baked at 120C for 30 minutes and remeasured
Obtained BER of 0.5%
Tried cycling 5K times with new SET voltages and rerunning experiment
  VWL = 3.5V, VBL = 2V
  Did not work!
  BER was ~10%

## Slide 4: Retention Figures

## Slide 5: Retention Figures

## Slide 6: Retention Figures (cycled)

## Slide 7: Retention Figures (cycled)

## Slide 8: Questions and Ideas
BL fine tuning seems to have been incorrect before
  No reason to use coarse tuning voltage as BL start voltage
  Should optimize BL start voltage in same way as SL start voltage
Ideas to improve FPPV algorithm yield
  “Ping-pong” SET/RESET approach
  FPPV has some issues with the low ranges on some cells but this can be fixed using slightly smarter approach
Should we compare to Ray’s algorithm?

## Slide 9: Appendix: Ranges
Range # | Rmin(n) (Ω) | Rmax(n) (Ω) | Rwmin(n) (Ω) | Rwmax(n) (Ω)
Range 0 | N.A. | 4300 | N.A. | 4200
Range 1 | 4375 | 4752 | 4540 | 4580
Range 2 | 4844 | 5304 | 5040 | 5090
Range 3 | 5419 | 6012 | 5670 | 5730
Range 4 | 6160 | 6988 | 6510 | 6600
Range 5 | 7189 | 8900 | 7710 | 7870
Range 6 | 9230 | 25000 | 11420 | 11930
Range 7 | 35000 | N.A. | 80000 | N.A.