## Slide 1: Method for finding good resistance control of RRAM
Akash Levy
Notes: Ask Binh about patent and also PCRAM project. Maybe also ask if Priyanka can join in on project

## Slide 2: Using E06 for testing instead of E01
1T4R I/O 1MBit device instead of 1T1R I/O 1MBit device
Wider transistor enables resistance levels < 3kOhm
Lowest resistance seems to be about 2.5 kOhm
However, 3.2kOhm seems like a good lower bound to prevent RRAM from getting stuck when the min LRS happens to be higher (device wear and variability!)

## Slide 3: Pulse Sweep Algorithm Trial 1
Using wafer 11, die 6: E06, 1T4R, only 1R used (rest are floating)
20 cells measured (10x each)
For each cell being tested, perform dynamic FORM
  For BL from 1V to 5V in steps of 0.1V
    For WL from 1V to 5V in steps of 0.2V
      FORM pulse (using PW=100ns, WL, BL from loop)
For each cell being tested, perform resistance control sweep 10 times
  For each pulse width PW being tested ([100ns, 1000ns])
    For WL from 0V to 4V in steps of 0.1V
      For BL from 0V to 5V in steps of 0.1V
        Read resistance
        If resistance < Rmax (100 kOhm)
          RESET pulse (using PW=1000ns, WL=3.5V, BL=2.5V)
        Read and record initial resistance Ri
        SET pulse (using PW, WL, BL from loop)
        Read and record final resistance Rf
        If Rf < Rmin (3.8 kOhm)
          Break out of WL loop (to prevent damage to cell)
This trial is qualitative, to see what parameters we should be sweeping! We will always assume RRAM’s only state variable is its current resistance 

## Slide 4: Some plots from trial 1
Chart: PW = 100 ns, WL = 2.0 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 465574.527 | 432290.322 | 471052.613 | 463900.245 | 454754.284 | 495231.474 | 498634.638 | 500857.484 | 461258.515 | 439047.41 | 418122.828 | 434338.835 | 445391.699 | 492988.388 | 18186.853 | 22770.127 | 50337.671 | 137238.027 | 36155.462 | 141440.158 | 111412.064 | 85006.322 | 65614.786 | 46198.06 | 83898.541 | 139614.538 | 148406.999 | 115078.436 | 113581.084 | 115414.008 | 142452.51 | 118512.503 | 93382.058 | 65522.209 | 41071.722 | 47193.357 | 91469.195 | 38882.349 | 117031.146 | 40590.203 | 66998.116 | 27976.065 | 214072.753 | 233865.819 | 112176.365 | 198742.581 | 204723.665 | 243104.88 | 221323.23 | 230217.704 | 164259.754
 | 446648.254 | 472266.172 | 447911.919 | 453038.901 | 426259.104 | 454991.909 | 526445.417 | 476922.224 | 451629.029 | 443294.272 | 444085.566 | 458103.782 | 425114.505 | 425946.33 | 526365.857 | 118625.522 | 574083.196 | 232911.839 | 293970.584 | 233646.182 | 130330.935 | 331805.6 | 307763.846 | 253841.818 | 176424.06 | 208548.213 | 129285.966 | 155427.009 | 110363.572 | 110700.313 | 104236.667 | 143834.973 | 108079.314 | 337954.916 | 283444.296 | 245037.541 | 181130.78 | 331932.086 | 295491.938 | 114688.134 | 251986.948 | 231672.452 | 325328.171 | 277615.457 | 247439.869 | 117922.669 | 107861.756 | 185027.824 | 272980.918 | 246337.337 | 259961.455
Chart: PW = 100 ns, WL = 2.1 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 173956.837 | 182660.152 | 178412.242 | 177557.289 | 177920.095 | 188512.868 | 184880.501 | 153956.763 | 236389.55 | 194015.36 | 256779.975 | 270773.812 | 239444.77 | 207085.065 | 196633.192 | 157088.392 | 136292.854 | 77819.426 | 42155.918 | 39646.266 | 46624.153 | 37573.645 | 26245.52 | 40816.624 | 33957.941 | 29716.349 | 15498.853 | 62817.229 | 19616.145 | 21652.011 | 71580.502 | 29545.941 | 76474.707 | 37437.943 | 23945.304 | 68949.106 | 29226.854 | 30684.476 | 22852.146 | 37765.944 | 24231.339 | 54859.332 | 30539.191 | 30063.132 | 70499.637 | 19060.296 | 27452.584 | 18102.819 | 41562.322 | 28467.916 | 20624.755
 | 177965.55 | 181338.25 | 182411.426 | 180980.191 | 178302.641 | 185649.153 | 190066.235 | 191603.243 | 169842.678 | 227838.271 | 145044.929 | 250230.878 | 193680.907 | 148217.535 | 169925.541 | 209136.766 | 200181.834 | 159673.765 | 112252.287 | 235160.599 | 345840.865 | 112962.214 | 195375.764 | 137791.822 | 295918.732 | 329763.623 | 237033.05 | 387124.957 | 304003.095 | 271216.597 | 159593.284 | 180230.985 | 221084.402 | 88252.268 | 234196.049 | 253453.907 | 221379.5 | 243308.67 | 238346.926 | 203574.944 | 226078.389 | 266464.965 | 285395.24 | 248836.436 | 424596.262 | 225070.35 | 186394.293 | 287586.78 | 212570.259 | 459918.533 | 133533.869
Seems to hit compliance current around 1.5V
Final resistance: ~50kOhm with lots of variation
Seems to hit compliance current around 2V
Final resistance: ~30kOhm with lots of variation
Orange is initial resistance
Blue is final resistance
X-axis: BL voltage (V)
Y-axis: Resistance (ohm)

## Slide 5: Some plots from trial 1
Chart: PW = 100 ns, WL = 2.2 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 139424.518 | 187528.335 | 179155.588 | 178705.171 | 180072.577 | 177856.497 | 138399.582 | 117283.36 | 168993.877 | 160364.834 | 161968.184 | 109290.03 | 106688.843 | 39483.57 | 109737.672 | 27946.659 | 151367.399 | 42270.521 | 38883.217 | 14300.642 | 13316.272 | 18982.283 | 15553.947 | 7836.43 | 23141.235 | 9797.671 | 11737.823 | 14750.823 | 22171.211 | 9120.955 | 9510.787 | 11238.885 | 15028.777 | 12327.07 | 12077.732 | 8029.037 | 9841.134 | 11717.013 | 7924.076 | 7277.34 | 10677.127 | 8559.713 | 11126.437 | 14151.43 | 9520.744 | 10047.611 | 11411.997 | 17572.978 | 14519.671 | 7454.831 | 18932.755
 | 200354.563 | 200585.333 | 184001.467 | 180539.279 | 179164.804 | 182526.138 | 179905.154 | 112466.142 | 156847.872 | 171760.716 | 156130.708 | 172338.634 | 112014.021 | 110339.098 | 249656.913 | 111726.566 | 255405.41 | 120284.706 | 369741.325 | 422638.411 | 133595.332 | 206483.502 | 469402.025 | 212921.121 | 289306.711 | 305442.73 | 308335.999 | 242613.793 | 316259.278 | 170767.003 | 235446.741 | 213914.979 | 284068.47 | 362280.352 | 178659.337 | 154901.661 | 153339.96 | 186344.431 | 226005.039 | 123382.476 | 206863.676 | 288587.579 | 254658.447 | 238249.102 | 257558.499 | 203183.043 | 275834.603 | 194383.51 | 199860.201 | 211588.828 | 132351.569
Chart: PW = 100 ns, WL = 2.3 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 237016.919 | 257330.15 | 257121.185 | 262192.379 | 260857.068 | 283075.708 | 279419.456 | 280138.624 | 222042.82 | 274790.022 | 259535.288 | 252096.38 | 135223.974 | 156869.064 | 84741.588 | 48985.459 | 51163.63 | 42132.461 | 17386.568 | 18026.272 | 11912.172 | 8193.976 | 9706.636 | 16162.397 | 7800.697 | 7686.694 | 8646.56 | 6642.024 | 6326.255 | 6101.622 | 6020.994 | 5961.509 | 5999.132 | 6198.912 | 6555.218 | 5421.277 | 7029.035 | 12543.538 | 5843.576 | 6191.144 | 6178.24 | 7057.993 | 8611.819 | 6425.386 | 5928.43 | 8075.409 | 7849.446 | 6342.164 | 7232.925 | 6974.312 | 6163.742
 | 250699.172 | 255293.087 | 262904.858 | 261778.547 | 274162.747 | 288253.207 | 266139.188 | 277947.771 | 265267.598 | 290005.287 | 288946.698 | 245538.499 | 167008.574 | 195639.147 | 142967.075 | 103156.142 | 180147.087 | 190014.389 | 215343.371 | 357850.952 | 185402.095 | 173757.236 | 197659.823 | 233380.035 | 355549.543 | 235160.599 | 271936.566 | 248145.027 | 217739.665 | 302156.976 | 334835.933 | 407888.885 | 497069.067 | 518143.841 | 394983.354 | 228675.967 | 251914.045 | 527881.611 | 355005.945 | 621402.788 | 334482.222 | 300151.97 | 564957.466 | 333138.535 | 450460.822 | 797929.477 | 625756.848 | 501434.342 | 218340.251 | 724560.508 | 310092.899
Seems to hit compliance current around 2.5V
Seems to hit compliance current around 2.5V
Orange is initial resistance
Blue is final resistance
X-axis: BL voltage (V)
Y-axis: Resistance (ohm)

## Slide 6: Some plots from trial 1
Chart: PW = 100 ns, WL = 2.2 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 139424.518 | 187528.335 | 179155.588 | 178705.171 | 180072.577 | 177856.497 | 138399.582 | 117283.36 | 168993.877 | 160364.834 | 161968.184 | 109290.03 | 106688.843 | 39483.57 | 109737.672 | 27946.659 | 151367.399 | 42270.521 | 38883.217 | 14300.642 | 13316.272 | 18982.283 | 15553.947 | 7836.43 | 23141.235 | 9797.671 | 11737.823 | 14750.823 | 22171.211 | 9120.955 | 9510.787 | 11238.885 | 15028.777 | 12327.07 | 12077.732 | 8029.037 | 9841.134 | 11717.013 | 7924.076 | 7277.34 | 10677.127 | 8559.713 | 11126.437 | 14151.43 | 9520.744 | 10047.611 | 11411.997 | 17572.978 | 14519.671 | 7454.831 | 18932.755
 | 200354.563 | 200585.333 | 184001.467 | 180539.279 | 179164.804 | 182526.138 | 179905.154 | 112466.142 | 156847.872 | 171760.716 | 156130.708 | 172338.634 | 112014.021 | 110339.098 | 249656.913 | 111726.566 | 255405.41 | 120284.706 | 369741.325 | 422638.411 | 133595.332 | 206483.502 | 469402.025 | 212921.121 | 289306.711 | 305442.73 | 308335.999 | 242613.793 | 316259.278 | 170767.003 | 235446.741 | 213914.979 | 284068.47 | 362280.352 | 178659.337 | 154901.661 | 153339.96 | 186344.431 | 226005.039 | 123382.476 | 206863.676 | 288587.579 | 254658.447 | 238249.102 | 257558.499 | 203183.043 | 275834.603 | 194383.51 | 199860.201 | 211588.828 | 132351.569
Chart: PW = 100 ns, WL = 2.3 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 237016.919 | 257330.15 | 257121.185 | 262192.379 | 260857.068 | 283075.708 | 279419.456 | 280138.624 | 222042.82 | 274790.022 | 259535.288 | 252096.38 | 135223.974 | 156869.064 | 84741.588 | 48985.459 | 51163.63 | 42132.461 | 17386.568 | 18026.272 | 11912.172 | 8193.976 | 9706.636 | 16162.397 | 7800.697 | 7686.694 | 8646.56 | 6642.024 | 6326.255 | 6101.622 | 6020.994 | 5961.509 | 5999.132 | 6198.912 | 6555.218 | 5421.277 | 7029.035 | 12543.538 | 5843.576 | 6191.144 | 6178.24 | 7057.993 | 8611.819 | 6425.386 | 5928.43 | 8075.409 | 7849.446 | 6342.164 | 7232.925 | 6974.312 | 6163.742
 | 250699.172 | 255293.087 | 262904.858 | 261778.547 | 274162.747 | 288253.207 | 266139.188 | 277947.771 | 265267.598 | 290005.287 | 288946.698 | 245538.499 | 167008.574 | 195639.147 | 142967.075 | 103156.142 | 180147.087 | 190014.389 | 215343.371 | 357850.952 | 185402.095 | 173757.236 | 197659.823 | 233380.035 | 355549.543 | 235160.599 | 271936.566 | 248145.027 | 217739.665 | 302156.976 | 334835.933 | 407888.885 | 497069.067 | 518143.841 | 394983.354 | 228675.967 | 251914.045 | 527881.611 | 355005.945 | 621402.788 | 334482.222 | 300151.97 | 564957.466 | 333138.535 | 450460.822 | 797929.477 | 625756.848 | 501434.342 | 218340.251 | 724560.508 | 310092.899
Seems to hit compliance current around 2.5V
Final resistance: around 6.5 kOhm, some variability
Seems to hit compliance current around 2.5V
Final resistance: around 11 kOhm, some variability
Orange is initial resistance
Blue is final resistance
X-axis: BL voltage (V)
Y-axis: Resistance (ohm)

## Slide 7: Some plots from trial 1
Seems to hit compliance current around 3V
Final resistance: around 4.5kOhm, low variability
Seems to hit compliance current around 2.5V
Final resistance: around 5kOhm, lower variability
Orange is initial resistance
Blue is final resistance
X-axis: BL voltage (V)
Y-axis: Resistance (ohm)
Chart: PW = 100 ns, WL = 2.4 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 627560.831 | 502809.721 | 561768.191 | 555673.708 | 599477.226 | 552851.239 | 593450.793 | 573421.593 | 655925.149 | 501723.27 | 455706.275 | 327530.882 | 536005.363 | 594159.451 | 459736.411 | 173230.07 | 86033.1 | 82521.004 | 56484.773 | 11831.163 | 7295.266 | 7737.135 | 7141.905 | 8895.96 | 6314.763 | 6115.42 | 8842.771 | 5696.163 | 4613.589 | 5414.088 | 5196.848 | 5980.282 | 5235.997 | 6300.495 | 6048.819 | 7286.231 | 5600.305 | 4294.257 | 4936.887 | 6496.141 | 6218.269 | 6112.276 | 6532.693 | 7016.475 | 6594.675 | 6429.74 | 4927.368 | 4510.77 | 4880.548 | 5587.171 | 6463.699
 | 688740.845 | 633381.087 | 517681.763 | 568461.362 | 591033.889 | 568275.863 | 584291.683 | 555319.324 | 566611.806 | 584487.787 | 459433.195 | 471052.613 | 580010.447 | 524147.913 | 603633.046 | 263441.764 | 216225.707 | 785866.922 | 106656.173 | 340166.36 | 785158.296 | 714014.43 | 371992.233 | 664180.495 | 624970.863 | 278058.72 | 215024.305 | 657907.543 | 332438.998 | 661029.137 | 555851.069 | 476987.538 | 450635.667 | 363717.972 | 492291.585 | 536748.782 | 590532.843 | 445163.994 | 657038.773 | 137411.287 | 339900.787 | 421921.641 | 695063.348 | 1251513.111 | 497779.47 | 464766.885 | 72397.349 | 258783.236 | 231011.716 | 281360.652 | 313216.136
Chart: PW = 100 ns, WL = 2.5 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 624522.614 | 494247.617 | 494037.299 | 545149.918 | 533705.617 | 580397.056 | 568554.157 | 506686.489 | 512049.826 | 429889.302 | 299172.261 | 373108.01 | 305335.623 | 29300.862 | 116347.005 | 35149.857 | 18366.868 | 20565.448 | 36941.201 | 10366.119 | 13100.006 | 14200.068 | 9527.906 | 11588.326 | 7619.982 | 8343.728 | 5292.446 | 5068.754 | 6105.087 | 4773.015 | 4806.071 | 5186.602 | 4778.692 | 4218.62 | 5208.895 | 4746.709 | 4532.1 | 5636.038 | 4591.202 | 4459.433 | 4914.783 | 4407.014 | 4515.747 | 5307.253 | 7400.532 | 4808.718 | 5638.008 | 5303.43 | 4549.552 | 4623.381 | 4822.948
 | 539994.239 | 449124.833 | 498491.906 | 609122.536 | 566980.754 | 539158.335 | 588736.091 | 614170.807 | 564957.466 | 570883.914 | 447911.919 | 305603.532 | 389811.218 | 236920.184 | 649685.237 | 110654.593 | 501073.65 | 365396.905 | 1033213.158 | 653831.902 | 431273.294 | 288468.072 | 733255.229 | 553114.627 | 466072.934 | 843536.462 | 534278.702 | 366088.217 | 488836.909 | 632690.754 | 298301.085 | 384220.987 | 234416.721 | 351921.121 | 369937.683 | 263222.76 | 357373.622 | 479548.809 | 230035.245 | 473164.382 | 237874.855 | 217698.836 | 233395.674 | 373828.837 | 222454.089 | 400662.971 | 326211.801 | 92369.162 | 140498.745 | 330263.928 | 222567.811

## Slide 8: Some plots from trial 1
Seems to hit compliance current around 3V
Final resistance: around 20kOhm, low variability
Nice BL tuning here!
Seems to hit compliance current around 2V
Final resistance: around 35kOhm, lots of variability
Orange is initial resistance
Blue is final resistance
X-axis: BL voltage (V)
Y-axis: Resistance (ohm)
Chart: PW = 1000 ns, WL = 1.5 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 286004.558 | 299429.459 | 401309.275 | 252736.637 | 316287.997 | 364364.818 | 257634.705 | 271660.833 | 425530.011 | 395386.902 | 437228.61 | 514926.509 | 345737.874 | 470479.943 | 336453.185 | 330076.136 | 300929.969 | 282089.861 | 186224.871 | 429306.438 | 663547.822 | 684813.697 | 1966662.407 | 933269.511 | 1393741.743 | 6164510.064 | 477118.22 | 399926.881 | 551276.165 | 587445.221 | 719620.325 | 362054.398 | 687788.795 | 916327.772 | 866408.455 | 497708.338 | 488562.628 | 636041.379 | 926812.622 | 616999.582 | 1097687.169 | 693540.908 | 567627.57 | 385539.434 | 286286.66 | 292809.036 | 599374.064 | 436352.181 | 506171.04 | 378418.433 | 371041.151
 | 297384.176 | 242884.492 | 264301.378 | 290950.087 | 288874.803 | 323665.403 | 238265.401 | 347219.952 | 392889.253 | 311674.58 | 634766.283 | 330326.573 | 366782.15 | 395521.601 | 338184.617 | 322675.876 | 261739.202 | 157543.144 | 76230.336 | 48892.628 | 46043.547 | 41934.12 | 32258.33 | 24729.936 | 16218.617 | 12061.545 | 19325.751 | 27086.23 | 25314.999 | 43543.583 | 71138.972 | 47240.724 | 29990.392 | 25187.765 | 42844.576 | 46808.372 | 39524.343 | 45196.908 | 46164.382 | 25324.939 | 35516.893 | 43436.605 | 53713.803 | 57382.805 | 30838.52 | 59638.775 | 41715.642 | 35218.809 | 11381.752 | 38478.139 | 28970.141
Chart: PW = 1000 ns, WL = 1.6 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 402701.26 | 371278.465 | 420698.533 | 461319.609 | 358403.305 | 373548.185 | 478428.984 | 417221.27 | 346494.563 | 440101.479 | 390466.73 | 502374.576 | 357924.501 | 406366.024 | 221986.212 | 263760.966 | 294542.366 | 321722.096 | 230965.759 | 1161374.199 | 111740.903 | 100362.033 | 497424.015 | 626995.97 | 691063.978 | 272938.135 | 199391.1 | 607740.824 | 309431.72 | 343013.921 | 372868.352 | 253085.568 | 317441.07 | 208174.27 | 596193.546 | 818172.919 | 738072.118 | 360145.105 | 283282.921 | 269391.565 | 208660.658 | 321306.588 | 203670.178 | 408319.248 | 602588.699 | 504484.782 | 671349.749 | 452450.386 | 254509.579 | 578469.148 | 354464.006
 | 299326.527 | 443859.193 | 379531.792 | 327469.292 | 426833.718 | 431006.45 | 464890.955 | 373307.961 | 586851.343 | 471562.824 | 469655.208 | 332661.259 | 566611.806 | 231380.034 | 192887.176 | 352455.306 | 250681.128 | 55145.967 | 66236.195 | 97718.037 | 98841.137 | 92049.369 | 71441.02 | 20043.991 | 30399.785 | 29718.378 | 18330.233 | 38665.233 | 38408.974 | 17861.904 | 21688.82 | 21907.502 | 20066.163 | 23094.435 | 16915.64 | 14521.487 | 29449.511 | 29916.461 | 25511.175 | 13277.793 | 20640.889 | 20910.917 | 19568.864 | 23241.608 | 12991.724 | 20060.269 | 19924.627 | 22515.04 | 13498.187 | 22650.774 | 21375.616

## Slide 9: Some plots from trial 1
Seems to hit compliance current around 3.5V
Final resistance: around 9kOhm, low variability
Nice BL tuning here!
Seems to hit compliance current around 3V
Final resistance: around 12kOhm, low variability
Nice BL tuning here!
Orange is initial resistance
Blue is final resistance
X-axis: BL voltage (V)
Y-axis: Resistance (ohm)
Chart: PW = 1000 ns, WL = 1.7 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 220175.97 | 249889.769 | 204880.218 | 204892.271 | 287278.415 | 270479.424 | 275050.425 | 207183.612 | 253067.179 | 253638.478 | 245192.792 | 275006.99 | 382449.023 | 363414.368 | 313413.429 | 243070.948 | 227258.492 | 134820.93 | 583020.209 | 540497.027 | 162254.907 | 2017936.842 | 531263.402 | 561134.652 | 434068.185 | 526365.857 | 173419.827 | 443802.636 | 444822.872 | 423666.603 | 361115.947 | 453865.398 | 236807.427 | 162724.903 | 351069.785 | 426415.663 | 342845.098 | 413359.028 | 307682.283 | 534032.943 | 289691.715 | 253952.868 | 314659.267 | 279643.799 | 320243.05 | 548584.473 | 437723.15 | 391960.75 | 166306.824 | 207097.378 | 273323.671
 | 250194.928 | 304827.888 | 182354.124 | 203301.641 | 244882.487 | 310313.92 | 211910.665 | 272064.016 | 259961.455 | 193347.604 | 283167.765 | 490558.165 | 383839.899 | 260116.771 | 226151.786 | 221014.257 | 138366.593 | 76113.725 | 114236.739 | 154770.878 | 48139.82 | 34489.233 | 27174.142 | 33894.822 | 29376.237 | 13135.132 | 15557.699 | 9634.942 | 17018.128 | 14987.776 | 11124.234 | 9920.657 | 13447.375 | 9124.085 | 15409.028 | 13810.655 | 8768.615 | 12523.693 | 14021.482 | 14031.028 | 11984.847 | 14615.757 | 19106.512 | 19036.544 | 11685.486 | 10665.977 | 11936.34 | 11063.316 | 11084.829 | 8360.091 | 16376.702
Chart: PW = 1000 ns, WL = 1.8 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 192524.667 | 180951.983 | 206581.477 | 233536.519 | 161953.121 | 196610.993 | 240486.337 | 153205.061 | 155572.8 | 172766.061 | 254546.78 | 215436.611 | 253989.906 | 217658.023 | 174707.253 | 172466.64 | 228196.531 | 237972.371 | 112480.67 | 606154.311 | 278147.542 | 272639.024 | 563039.57 | 736044.448 | 242023.738 | 364631.836 | 290489.032 | 179960.927 | 187366.924 | 304162.384 | 363414.368 | 46852.448 | 94126.53 | 227987.409 | 130389.484 | 173316.272 | 26519.695 | 173376.664 | 136016.085 | 112458.879 | 130786.073 | 163381.36 | 126579.587 | 182182.434 | 132659.071 | 102802.951 | 74194.02 | 124254.002 | 102431.079 | 106555.021 | 100748.141
 | 190253.114 | 177024.843 | 199288.421 | 191540.021 | 175703.162 | 257349.163 | 208199.157 | 146638.762 | 156516.597 | 236678.692 | 248552.316 | 235351.283 | 256213.299 | 233473.9 | 155440.882 | 297079.791 | 196655.397 | 104267.871 | 68656.891 | 91026.945 | 38262.558 | 39910.211 | 19579.864 | 21991.742 | 14696.3 | 12222.557 | 15742.069 | 12575.149 | 9953.772 | 11172.765 | 11908.466 | 9835.187 | 9043.325 | 11140.352 | 9046.284 | 8121.069 | 8160.896 | 10174.17 | 8839.517 | 7185.044 | 9110.791 | 9299.461 | 8520.471 | 10540.447 | 7881.507 | 7345.639 | 9983.244 | 10722.95 | 7623.601 | 8944.094 | 7759.595

## Slide 10: Some plots from trial 1
Seems to hit compliance current around 3V
Final resistance: around 6.5kOhm, low variability
Problem: not RESETing fully! Endurance???
Seems to hit compliance current around 3V
Final resistance: around 7.5kOhm, low variability
Nice BL tuning here! Problem: not RESETing fully!
Orange is initial resistance
Blue is final resistance
X-axis: BL voltage (V)
Y-axis: Resistance (ohm)
Chart: PW = 1000 ns, WL = 1.9 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 99012.536 | 81984.889 | 101951.35 | 88616.019 | 143805.28 | 137346.263 | 142150.187 | 130526.304 | 138968.355 | 131566.649 | 110070.599 | 121391.466 | 131081.401 | 156383.075 | 111511.941 | 102572.858 | 79654.303 | 151472.726 | 71577.56 | 105997.26 | 197167.491 | 124298.345 | 92241.956 | 140549.771 | 101683.472 | 146140.388 | 95053.873 | 60941.055 | 54547.455 | 132957.852 | 97674.191 | 119332.714 | 108139.716 | 80199.038 | 74037.881 | 82581.659 | 76407.6 | 75046.089 | 47379.532 | 30288.752 | 59713.415 | 56283.052 | 58730.677 | 49688.486 | 68792.496 | 39649.426 | 62320.428 | 54262.765 | 59054.309 | 50724.01 | 40964
 | 95308.778 | 74303.233 | 111992.41 | 125110.957 | 157635.838 | 140947.913 | 130369.962 | 127553.062 | 128375.803 | 137715.547 | 123891.578 | 125557.459 | 102684.748 | 140589.484 | 100474.945 | 84671.546 | 54868.838 | 30718.846 | 34211.441 | 17413.08 | 25720.857 | 14442.665 | 15115.786 | 9896.978 | 9374.071 | 11481.593 | 9295.018 | 7110.673 | 7204.424 | 7248.942 | 7212.853 | 9508.502 | 8277.046 | 8021.16 | 7387.504 | 7116.398 | 7735.778 | 7847.943 | 5897.202 | 6150.224 | 8178.737 | 7254.377 | 7885.469 | 7124.783 | 7407.111 | 7441.866 | 6134.571 | 7136.14 | 6670.991 | 7519.564 | 7160.081
Chart: PW = 1000 ns, WL = 2 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 41915.448 | 81900.064 | 82992.924 | 65639.517 | 67882.127 | 49919.94 | 105900.574 | 96746.312 | 93119.91 | 64701.828 | 150699.371 | 129845.061 | 116413.114 | 117568.403 | 124191.974 | 136919.722 | 104861.176 | 96049.97 | 119607.278 | 72136.447 | 118848.152 | 57638.249 | 82308.442 | 74099.312 | 70658.391 | 87307.648 | 80199.038 | 78385.111 | 59356.228 | 53664.973 | 58240.625 | 46481.045 | 66368.72 | 67284.151 | 61583.254 | 59790.296 | 63815.095 | 57265.814 | 49471.111 | 72859.26 | 44658.539 | 52238.715 | 39351.525 | 41833.89 | 35682.087 | 75083.299 | 42418.786 | 72531.53 | 56222.181 | 57772.096 | 45715.39
 | 45942.728 | 74431.851 | 77769.036 | 71861.105 | 65710.104 | 51549.828 | 93090.044 | 98981.584 | 89683.902 | 72108.071 | 116149.129 | 118917.134 | 120060.804 | 124134.433 | 51856.06 | 71657.081 | 83446.274 | 28059.23 | 22480.454 | 12538.39 | 16714.324 | 22639.731 | 10347.211 | 14365.76 | 10004.263 | 8790.547 | 8218.008 | 10774.431 | 7402.073 | 7661.652 | 6999.343 | 6347.388 | 6576.172 | 6996.742 | 5711.378 | 5746.157 | 5438.138 | 5533.381 | 6322.672 | 7130.369 | 5950.754 | 5897.072 | 6875.868 | 6321.835 | 6749.041 | 6178.185 | 6072.018 | 6838.124 | 5717.792 | 6003.31 | 6715.468

## Slide 11: Some plots from trial 1
Seems to hit compliance current around 3V
Final resistance: around 5kOhm, low variability
Nice BL tuning here! Problem: not RESETing fully!
Seems to hit compliance current around 3V
Final resistance: around 5.5kOhm, low variability
Problem: not RESETing fully!
Orange is initial resistance
Blue is final resistance
X-axis: BL voltage (V)
Y-axis: Resistance (ohm)
Chart: PW = 1000 ns, WL = 2.1 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 47633.536 | 64005.073 | 74358.754 | 61802.897 | 85700.746 | 75700.153 | 63137.208 | 170066.592 | 145087.223 | 148135.584 | 94581.507 | 130992.663 | 126985.705 | 126299.595 | 126773.092 | 144037.214 | 128262.343 | 147103.259 | 84836.537 | 221224.827 | 236614.377 | 153515.684 | 93706.153 | 162907.569 | 117453.428 | 118827.878 | 121816.03 | 108223.72 | 123570.706 | 86967.565 | 93422.134 | 64686.206 | 64524.428 | 58607.146 | 52102.742 | 56597.671 | 92854.279 | 66156.933 | 112169.14 | 67057.452 | 92440.257 | 59553.118 | 77048.204 | 64776.434 | 57392.26 | 75529.428 | 48801.515 | 47014.985 | 44060.825 | 26622.468 | 50177.404
 | 46600.449 | 60379.026 | 65886.614 | 72131.965 | 70773.252 | 74825.214 | 66718.337 | 154331.968 | 150289.703 | 108533.98 | 94622.619 | 116409.223 | 113233.979 | 105184.187 | 50560.543 | 108863.036 | 47190.799 | 71895.223 | 21800.819 | 48006.452 | 27031.573 | 11418.319 | 14523.122 | 9169.17 | 8465.55 | 7432.29 | 7220.404 | 6498.577 | 6823.923 | 5639.414 | 6662.314 | 6402.908 | 5562.526 | 5512.938 | 5583.911 | 6131.202 | 5870.376 | 5126.499 | 6110.281 | 5373.311 | 5528.945 | 5110.403 | 6117.074 | 5608.828 | 5815.136 | 5228.53 | 5690.365 | 5638.027 | 5189.833 | 5559.888 | 5843.772
Chart: PW = 1000 ns, WL = 2.2 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 36530.502 | 60421.971 | 122187.824 | 116976.119 | 116991.836 | 119891.361 | 127763.615 | 127115.471 | 101078.53 | 101172.485 | 97313.961 | 97652.283 | 117850.847 | 122708.707 | 102512.479 | 111988.809 | 80880.664 | 51735.129 | 89474.247 | 102988.379 | 81465.22 | 135213.475 | 131800.647 | 133888.056 | 165784.369 | 107688.34 | 121180.291 | 93582.783 | 79016.403 | 112068.083 | 52105.86 | 50895.973 | 60268.279 | 87347.06 | 57429.167 | 66741.35 | 67273.754 | 73416.75 | 60559.597 | 66795.107 | 81963.666 | 105035.102 | 89584.712 | 48742.098 | 81301.682 | 75278.033 | 98441.649 | 59141.549 | 112597.031 | 76143.676 | 59591.837
 | 35444.966 | 52543.698 | 122033.703 | 116284.854 | 116991.836 | 126116.664 | 114574.951 | 121527.004 | 104127.597 | 103499.464 | 118146.674 | 137890.015 | 131636.264 | 118982.132 | 86645.207 | 36322.496 | 40973.156 | 25367.732 | 37064.245 | 27248.124 | 23763.794 | 12850.37 | 18228.829 | 8302.518 | 7643.175 | 6724.934 | 7896.857 | 6373.569 | 5422.078 | 5533.855 | 5238.564 | 4651.419 | 5349.05 | 5172.975 | 4764.487 | 4756.192 | 4786.33 | 5124.546 | 4859.785 | 5430.007 | 4791.848 | 5550.806 | 5544.329 | 5350.973 | 5058.301 | 4900.49 | 5908.166 | 4466.06 | 4625.002 | 5340.798 | 4562.012

## Slide 12: Some plots from trial 1
Seems to hit compliance current around 3V
Final resistance: around 4.25kOhm, low variability
Seems to hit compliance current around 3V
Final resistance: around 4.5kOhm, low variability
Orange is initial resistance
Blue is final resistance
X-axis: BL voltage (V)
Y-axis: Resistance (ohm)
Chart: PW = 1000 ns, WL = 2.3 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 55789.017 | 98394.372 | 182440.091 | 162307.835 | 174462.222 | 206031.571 | 182001.556 | 203301.641 | 182497.447 | 222170.292 | 180829.852 | 181253.319 | 172441.024 | 132871.625 | 159352.328 | 156446.294 | 202816.265 | 118994.327 | 254621.214 | 135134.783 | 154099.807 | 186185.052 | 198890.117 | 266934.668 | 222141.952 | 147352.196 | 96948.282 | 110784.82 | 113874.451 | 117556.499 | 230720.962 | 142307.002 | 130933.57 | 193584.023 | 73056.404 | 123640.892 | 130282.184 | 95717.379 | 141308.174 | 95775.285 | 113736.863 | 64380.112 | 60411.491 | 168846.413 | 140063.694 | 154174.842 | 67779.089 | 138350.105 | 107389.51 | 216763.983 | 98695.494
 | 52362.014 | 109994.125 | 158223.043 | 171060.547 | 201455.476 | 245434.685 | 242428.038 | 180464.444 | 196311.788 | 154249.949 | 189641.934 | 188482.264 | 142528.292 | 105069.956 | 219773.074 | 85774.615 | 114616.426 | 47042.926 | 12921.307 | 13418.001 | 12468.146 | 10960.059 | 8219.967 | 6886.963 | 5959.255 | 5324.241 | 5701.73 | 6225.716 | 5148.78 | 5667.365 | 4437.355 | 5569.909 | 4852.818 | 5373.079 | 4698.53 | 4577.565 | 4698.423 | 5700.722 | 4639.226 | 4474.368 | 4750.393 | 4720.212 | 4885.902 | 5072.216 | 4406.54 | 4572.391 | 4392.762 | 5392.679 | 4485.258 | 4236.363 | 4460.278
Chart: PW = 1000 ns, WL = 2.4 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 65799.484 | 143692.556 | 102190.652 | 107758.306 | 98539.127 | 104665.804 | 104452.361 | 104258.508 | 226666.905 | 198278.705 | 214217.583 | 193799.452 | 236181.164 | 217345.628 | 176263.35 | 158698.858 | 121256.229 | 334289.603 | 169158.028 | 287539.296 | 171085.755 | 120856.516 | 197156.33 | 140856.711 | 304481.463 | 145529.765 | 137313.774 | 164391.552 | 84470.304 | 148527.244 | 141067.796 | 78695.046 | 159476.366 | 109513.393 | 122140.69 | 130977.885 | 145736.804 | 185382.359 | 236694.776 | 186085.578 | 248215.764 | 170324.407 | 202969.914 | 137210.995 | 213731.203 | 140868.104 | 133457.119 | 275769.084 | 169768.171 | 83526.32 | 141999.506
 | 60238.051 | 142103.789 | 100214.76 | 109896.948 | 106000.486 | 112735.522 | 117204.426 | 104174.313 | 180436.397 | 293425.736 | 231149.698 | 235033.648 | 188309.027 | 178934.692 | 149940.327 | 87417.213 | 41248.776 | 76669.984 | 37136.961 | 17265.903 | 13438.917 | 12257.528 | 8485.7 | 7014.737 | 5524.463 | 5440.024 | 5504.383 | 5602.954 | 5875 | 5125.187 | 4337.64 | 4793.404 | 4374.319 | 4233.176 | 4470.549 | 4119.438 | 4295.851 | 4905.383 | 4303.771 | 4126.847 | 4867.915 | 5028.745 | 4263.85 | 4301.283 | 4177.724 | 4285.27 | 5305.595 | 4073.561 | 5235.714 | 4064.221 | 4589.019

## Slide 13: Some plots from trial 1
Seems to hit compliance current around 3V
Final resistance: around 4kOhm, low variability
Seems to hit compliance current around 3V
Final resistance: around 4.1kOhm, low variability
Orange is initial resistance
Blue is final resistance
X-axis: BL voltage (V)
Y-axis: Resistance (ohm)
Chart: PW = 1000 ns, WL = 2.5 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 159374.203 | 151433.211 | 140351.543 | 152147.643 | 128893.639 | 112819.511 | 124596.263 | 117795.047 | 115029.028 | 160357.451 | 145614.945 | 156996.342 | 183381.444 | 142138.585 | 150973.726 | 118415.8 | 141227.957 | 174165.606 | 240685.759 | 344916.157 | 166290.944 | 280341.558 | 221986.212 | 232616.285 | 216763.983 | 150037.213 | 138907.39 | 203135.642 | 181546.196 | 228811.171 | 146379.922 | 117826.926 | 232151.146 | 131556.71 | 160062.676 | 201420.525 | 169569.806 | 83548.36 | 121412.624 | 243887.936 | 86182.116 | 225536.726 | 209728.651 | 228871.314 | 93698.59 | 210705.608 | 156081.732 | 232616.285 | 178448.805 | 168259.121 | 110091.474
 | 148533.578 | 134027.164 | 134352.874 | 124249.569 | 118730.661 | 137238.027 | 141199.33 | 135666.416 | 147121.9 | 142879.102 | 180473.795 | 217916.767 | 157010.496 | 132851.352 | 138399.582 | 150205.445 | 62830.827 | 16761.137 | 24202.378 | 13268.991 | 11486.288 | 11050.119 | 8206.448 | 7495.936 | 6866.853 | 4812.093 | 5465.471 | 4575.659 | 4363.605 | 4563.878 | 4261.706 | 5037.182 | 4726.432 | 4067.748 | 4197.531 | 4374.742 | 4208.888 | 4100.21 | 4250.539 | 4369.183 | 3924.365 | 4138.321 | 4385.798 | 3921.246 | 4035.847 | 4133.297 | 4039.845 | 4009.075 | 4891.268 | 4131.885 | 4407.214
Chart: PW = 1000 ns, WL = 2.6 V
| 0 | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4 | 4.0999999999999996 | 4.2 | 4.3 | 4.4000000000000004 | 4.5 | 4.5999999999999996 | 4.7 | 4.8 | 4.9000000000000004 | 5
 | 198561.298 | 214481.414 | 253712.382 | 205824.59 | 212713.063 | 217549.262 | 216279.414 | 271682.023 | 251659.219 | 210782.117 | 205327.107 | 282639.253 | 181376.023 | 139681.728 | 158691.627 | 250176.957 | 192961.98 | 422946.344 | 270185.676 | 335384.051 | 547549.571 | 393510.702 | 279464.296 | 481271.659 | 214481.414 | 675516.386 | 167184.938 | 185520.601 | 222909.675 | 337104.469 | 317470.005 | 319948.871 | 231103.686 | 324509.774 | 206863.676 | 201618.739 | 199573.901 | 256874.665 | 156883.196 | 144623.339 | 281701.999 | 305335.623 | 308663.9 | 383459.567 | 254398.041 | 286710.858 | 192152.916 | 166473.751 | 133918.944 | 149946.782 | 165839.626
 | 160394.374 | 225084.895 | 232771.746 | 244127.26 | 197480.509 | 193326.14 | 242901.431 | 230996.395 | 211255.152 | 197290.344 | 265106.071 | 186554.031 | 148470.261 | 155642.32 | 54468.975 | 75018.611 | 62448.928 | 51533.048 | 24725.723 | 31202.926 | 9839.104 | 8715.429 | 6944.359 | 5572.627 | 5664.25 | 4914.776 | 4781.815 | 4423.761 | 4697.421 | 5052.014 | 4492.692 | 4169.911 | 4172.274 | 4513.003 | 4275.564 | 4480.014 | 4586.813 | 4003.071 | 4720.494 | 4146.445 | 3944.007 | 3909.928 | 4341.154 | 4145.784 | 4604.051 | 3956.489 | 4235.879 | 3995.421 | 3809.603 | 3900.881 | 3891.271

## Slide 14: Observations and changes from trial 1
We need to try higher WL voltages:
  Below 1.5V, we see no change in resistance, so we can eliminate these tests
  In general, can probably eliminate anything below threshold voltage of select transistor…
  Try WL from 1V to 4V
We need to reduce the minimum resistance
  3.8 kOhm -> 3.3 kOhm so we can see how the lower target will work out
10ns pulse width does not work with NI setup
  Try scaling PW in multiples of 2: 40 ns, 100 ns, 200 ns, 400 ns, 800 ns, 1600 ns

## Slide 15: Pulse Sweep Algorithm Trial 2
Using wafer 11, die 6: E06, 1T4R, only 1R used (rest are floating)
20 cells measured (5x each)
For each cell being tested, perform dynamic FORM
  For BL from 1V to 5V in steps of 0.1V
    For WL from 1V to 5V in steps of 0.2V
      FORM pulse (using PW=100ns, WL, BL from loop)
For each cell being tested, perform resistance control sweep 5 times
  For each pulse width PW being tested ([40ns, 100ns, 200ns, 400ns, 800ns, 1600ns])
    For WL from 1V to 4V in steps of 0.1V
      For BL from 0V to 5V in steps of 0.1V
        Read resistance
        If resistance < Rmax (100 kOhm)
          RESET pulse (using PW=1000ns, WL=3.5V, SL=2.5V)
        Read and record initial resistance Ri
        SET pulse (using PW, WL, BL from loop)
        Read and record final resistance Rf
        If Rf < Rmin (3.2 kOhm)
          Break out of WL loop (to prevent damage to cell)
This trial is quantitative, to see how to best program the RRAM. Just finished running!

## Slide 16: Our Algorithm v1: state-dependent retry
This is what is currently planned for implementation
RESET pulse (using PW=1000ns, WL=3.5V, BL=3V)
While i < max_i:
  Optimal SET pulse to maximize probability of landing in target distribution (pulse parameters from lookup table)
  Read resistance
  If landed in target distribution, done!
  Else, RESET and increment i

## Slide 17: Our Algorithm v2: target Rf from Ri
Modification from v1
Start from Ri and instead of RESETing to HRS, go directly to Rf
Use idea of fine, medium, coarse pulses
Could be unidirectional (SET only) or bidirectional (SET and RESET)
This might end up consuming more power though depending on the power metric used…

## Slide 18: Our Algorithm v3: optimal target Rf from Ri
Start from Ri and instead of RESETing to HRS, go directly to Rf
Use optimal pulse
Could be unidirectional (SET only) or bidirectional (SET and RESET)
This might end up consuming more power though depending on the power metric we use…

## Slide 19: ISPP Algorithm (as done right now)
RESET (using PW=1000ns, WL=3.5V, BL=3V)
For BL from 0V to 5V in steps of 0.01V (need to tune step size for fair comparison)
  Pulse (using PW=100ns, WL=3.5V, BL from loop)
  Read resistance
  If resistance in window, done!
  If resistance below window
    RESET (using PW=1000ns, WL=3.5V, BL=3V)
Not tested yet

## Slide 20: Ping-Pong Algorithm (as done right now)
While resistance read is not in target range
  Perform dynamic SET if below
    BL from 0.4V to 3.3V
      WL from 1.4V to 3.3V
  Perform dynamic RESET if above
    SL from 1.5V to 3.3V
      WL from 1.4V to 3.3V
  Quit if unsuccessful after 10 tries

## Slide 21: Energy & Delay Benchmarking
Need to develop a reasonable cost model
There is an energy/delay tradeoff as shown by the PW findings
READ operation:
  WL=2V, BL=0.2V (need to assume WL is completely on in this scenario)
  (Do we need a higher read WL voltage for I/O transistors?)
  Delay = 25 ns (not possible with NI, but works with integrated peripherals)
  Energy = VBL^2 / R * Delay
SET/RESET operation (many ways to do energy estimate!):
  Delay = PW
  Initial-Counts Energy Estimate = VBL^2 / Ri * Delay
  Final-Counts Energy Estimate = VBL^2 / Rf * Delay
  Worst-Case Energy Estimate = VBL^2 / min(Ri, Rf) * Delay
  Best-Case Energy Estimate = VBL^2 / max(Ri, Rf) * Delay
  Linear Resistance Ramp Energy Estimate = VBL^2 / avg(Ri, Rf) * Delay
  Linear Conductance Ramp Energy Estimate = avg(Worst-Case, Best-Case)
  Which energy estimate is best to use?

## Slide 22: Some Questions
Should we make WL always on outside loop to be consistent?
Should we modify ping-pong algorithm for I/O?
Should we increase READ WL voltage for I/O?
  This might improve the resistance window’s lower bound…
Can we/should we calibrate our findings to an RRAM model as done in Alessandro Grossi’s paper?

## Slide 23: Next Steps
Python statistical analysis:
  Average final resistance given PW, BL voltage, WL voltage
  Average final stdev resistance given PW, BL voltage, WL voltage
  Statistics of these values across cells
  Need to make sure things don’t get messed up across iterations (account for outliers)
Fitting of final resistance to PW, BL, WL with polynomial function
Determine probability of missing target and optimize w.r.t. expected number of trials

## Slide 24: Notes
POLYFITN MATLAB can help fit to data
Is this the first time PW has been explored?
FORMing analysis on E06 1T4R I/O 1R (has this been done?)