## Slide 1: Updates 7/18/20
Akash Levy

## Slide 2: Overview
Sweep plot for FPPV
Sweep plots for VWL and VBL
Retention distribution plots
Retention BER plot
ISPP optimization results
SDCFC optimization results
ISPP/FPPV evaluation on chip 1

## Slide 3: TODO List (In Order)
Evaluate ISPP on 4K more cells and add to previously collected data
Optimize SDR SL over 256 cells
  Sweep step size from 0.02 to 0.14 in steps of 0.02 (7)
  Sweep start voltage from 0 to 1 in steps of 0.2 (6)
  Total: 42
Optimize SDR BL over 256 cells
  Sweep step size from 0.02 to 0.14 in steps of 0.02 (7)
  Sweep start voltage from 0 to 1 in steps of 0.2 (6)
  Total: 42
Evaluate SDCFC on 8K cells
Evaluate FPPVv2 on 8K cells (with 2000 attempts)
Redo sweeps on 50 cells with 10 per cell and using consistent step sizes
  7.5 kOhm slope measurement
Endurance testing

## Slide 4: Sweep Plots: FPPV VWL

## Slide 5: Sweep Plots: VWL SET/RST (REDO STEP)
Notes: Slope @ resistance is the key!!!

## Slide 6: Sweep Plots: VBL/VSL SET/RST (REDO STEP)
Notes: Slope @ resistance is the key!!!

## Slide 7: ISPP Optimization Results

## Slide 8: Algorithm evaluation on 4 WLs (TODO)

## Slide 9: Algorithm evaluation on 4 WLs (TODO)
Chip # | Cycles | ISPP | FPPV | SDCFC
1 | 300 |  |  | 
2 | 300 |  |  | 
1 | 10k |  |  | 
2 | 10k |  |  | 

## Slide 10: Resistance Ranges
 | Rmin | Rmax | Rwmin | Rwmax
Range 0 | N/A | 4.3k | N/A | 4.2k
Range 1 | 4.38k | 4.75k | 4.54k | 4.58k
Range 2 | 4.84k | 5.3k | 5.04k | 5.09k
Range 3 | 5.42k | 6.01k | 5.67k | 5.73k
Range 4 | 6.16k | 6.99k | 6.51k | 6.59k
Range 5 | 7.19k | 8.9k | 7.71k | 7.87k
Range 6 | 9.2k | 25k | 11.42k | 11.93k
Range 7 | 20k | N/A | 80k | N/A

## Slide 11: Retention model plot

## Slide 12: Retention BER plot